## Slide 1: Plan – 6 samples per run
First Run
  Thin samples Ru series (4) NT083,84,86,76
  Thickness series (2) 75, 74
  Set 7T (field on always)
  H+(σ+, σ-), H-(σ+, σ-) for each temp (370K, 300K, 200K, 100K, 50K, 10K, 4K)
  Angle scan of NT075 (5 angles)
  NT075 Linear dichroism (s, p ) + angle scan
  NT075 Ru and Ga edge

## Slide 2: Plan
Second run
  Thickness series (2) NT073, 72
  Ru content thick samples (4), 59,58,63,55
  H+(σ+, σ-), H-(σ+, σ-) for each temp (400K, 300K, 200K, 100K, 50K, 10K, 4K)
  Florescence
  Control samples to go on the backside

## Slide 3: Plan
Third run
  Capping series (4), MgO/AlOx, AlOx, Mg/MgO, Al/AlOx
  Mn2Ga on MRG (2) – 2 thickness of MRG YC267,272
Fourth run
  Cubic Mn2Ga on V composition (5) ,Mn2Ga, Mn2.25Ga,Mn2.5Ga,Mn2.75Ga, Mn3Ga

## Slide 4: Ultra thin samples – Ru conc

## Slide 13: Thickness dependence

## Slide 14
0.08µB

## Slide 17
not fully switched (?)

## Slide 20
not fully switched (?)

## Slide 23
not fully switched (?)

## Slide 26
not fully switched (?)

## Slide 29: Ru composition series

## Slide 30
0.26µB

## Slide 31
NT046

## Slide 32
0.11µB

## Slide 33
NT055

## Slide 34
0.09µB

## Slide 35
NT063

## Slide 36
not fully switched (?)

## Slide 37
NT058

## Slide 38
0.10µB

## Slide 39
NT059

## Slide 40: Mn2Ga on MRG

## Slide 41
0.96µB

## Slide 45: Cubic Mn2Ga / Mn3Ga on V

## Slide 46
YC330 Mn2Ga– V(0.1A 30min)/Mn2Ga (0.1A 30min) T350
YC343 Mn2.25Ga– V(0.1A 30min)/Mn2Ga (0.09A) Mn3Ga (0.03A) (25min) T350
YC342 Mn2.5Ga– V(0.1A 30min)/Mn2Ga (0.06A) Mn3Ga (0.06A) (25min) T350
YC344 Mn2.75Ga– V(0.1A 30min)/Mn2Ga (0.03A) Mn3Ga (0.09A) (25min) T350
YC341 Mn3Ga– V(0.1A 30min)/Mn3Ga (0.1A 30min) T350

## Slide 48: Pure materials , Mn, Ru, and/or oxides
Ru metal
Mn metal
Mn(II)oxide
Mn(IV)oxide
Ga(III)oxide

## Slide 49: MRG capped with diff tunnel barriers

## Slide 50: Lattice Parameters
Sample | c (A)
NT046 | 6.06364
NT055 | 6.0724
NT063 | 6.06488
NT058 | 6.07324
NT059 | 6.06728
NT072 | 6.06531
NT073 | 6.07041
NT074 | 6.08917
NT075 | 6.12888
NT076 | 6.17176
NT083 | 6.20556
NT084 | 6.19568
NT086 | 6.19044
NT088 | 6.07584
YC267 | 6.0714
YC272 | 6.00936
YC330 | 5.83496
YC343 | 5.82628
YC342 | 5.83132
YC344 | 5.82516
YC341 | 5.8372
YC268 | 6.0044